Quality Clause 240306 - Hub Radiography (07/01/2025 - Rev A)

The thin web sections of the hub body, between the blade ports, shall be subject to radiographic inspection (RT) per T9074-AS-GIB-010/271.

RT acceptance criteria shall be in accordance with Table XIX, Criticality Level 1, of S9074-AR-GIB-010/278.